12 kinds of fiber identification methods (2) -- combustion method

One of the common methods for identifying natural fibers. Because the chemical composition of the fibers is different, the combustion characteristics are also different. Cellulosic fibers and protein fibers can be distinguished based on how easily the fibers burn, whether they are thermoplastic, the odor produced during combustion, and the characteristics of the ashes after combustion. Cellulose fibers such as cotton, hemp and viscose burn quickly in contact with the flame, and continue to burn after leaving the flame, with the smell of burning paper, leaving a small amount of soft gray ash after burning; Protein fibers such as wool and silk burn slowly when they come into contact with the flame, and continue to burn slowly after leaving the flame, with a smell of burning feathers, leaving black brittle ash after burning.

Characteristics of various fibers during and after combustion

| Types of fibers | Approach the flame | In the flames | Leave the flames | Burnt smell | Residue form |
| --- | --- | --- | --- | --- | --- |

| Fiber Types | Approaching Flame | In Flame | Leaving Flame | Burning Odor | Residue Form |
| --- | --- | --- | --- | --- | --- |
| Tencel Fiber | Does not melt or shrink | Burns rapidly | Continues to burn | Smells like burning paper | Ashy black ash |
| Modal Fiber | Does not melt or shrink | Burns rapidly | Continues to burn | Smells like burning paper | Ashy black ash |
| Soybean Protein Fiber | Shrinks | Burns without melting or fusing, with black smoke | Does not spread easily | Smells like burning hair | Brittle black ash |
| Bamboo Fiber | Does not melt or shrink | Burns rapidly | Continues to burn | Smells like burning paper | Ashy black ash |
| Chitin Fiber | Does not melt or shrink | Burns rapidly | Continues to burn | Smells like burning paper | Ashy black ash |
| Viscose Fiber | Does not melt or shrink | Burns rapidly | Continues to burn | Smells like burning paper | A small amount of off-white ash |
| Cotton Fiber | Does not melt or shrink | Burns rapidly | Continues to burn | Smells like burning paper | A small amount of off-white ash |

| Silk | Shrinkage | Gradual Burning | Not Easily Flammable | Smell of Burning Hair | Brittle Black Ash |
| --- | --- | --- | --- | --- | --- |
| Wool Fiber | Shrinkage | Gradual Burning | Not Easily Flammable | Smell of Burning Hair | Brittle Black Ash |
| Polyester Fiber | Shrinkage and Melting | Melts First and Then Burns, with Solution Dropping | Flammable and Can Spread | Special Aromatic Smell | Glassy Black Brown Hard Ball |